DIAMONDBOND-001™ TECHNICAL DATA  SHEET

| Clinical Indications | Universal Adhesive Bonding Resin Material - Enamel, Dentin, Resin, Ceramic & Metal Substrates - For : Esthetic Fillings; Class I, II, III, IV, V, Metal-Free Crown& Bridge, Inlays/Onlays, Laminate-Veneers, Implant-Superstructures, Pins, Post/Core, Splints, Ortho-Brackets, Pit&Fissure Sealant & Flowable Cavity Liner/Base. |
| --- | --- |
| Composition | PolyCrystalline Matrix/Synthetic Collagen Primer, Self-Etch-Prime&Bond - Single Step Adhesive Application |
| Mode of Cure | Dual-Cure : Visible Light Cure (Base) + Self/Auto-Cure (Catalyst), Cure - Light, Auto or Dual |
| Delivery System | 3cc & 7cc vials of ; Adhesive - Catalyst(SC) & Base(VLC), 7cc Conditioner |

PROPERTY ------------------- STD. SPEC. #

DIAMOND

BOND-001

ISO/ADA…..

| Criteria | ** Zinc Phosphate | **Poly-carboxylate | ** Glass Ionomer |
| --- | --- | --- | --- |
| Bond-Strength (MPa) - Dentin 3107(I)/ 8(A)/ 9(A)/(D) | 37 | 5 | 2 | 3 | 8 |
| Bond (MPa) - Enamel 3107(I)/ 8(A)/ 9(A)/(D) | 27 | 7 | 3 | 4 | 6 |
| Bond (MPa) - Composite 3107(I)/ 8(A)/ 9(A)/(D) | 34 | 8 | 3 | 4 | 8 |
| Bond (MPa)- Porcelain 3107(I)/ 8(A)/9(A)/(D) | 30 | 4 | 3 | 4 | 7 |
| Bond (MPa)- Gold Alloys 3107(I)/8(A)/ 9(A)/(D) | 23 | 4 | 4 | 5 | 5 |
| Bond (MPa) - Titanium 3107(I)/8(A)/ 9(A)/(D) | 27 | 5 | 5 | 6 | 7 |
| Bond (MPa) - Chrome-Cobalt 3107(I)/8(A)/ 9(A)/(D | 28 | 5 | 6 | 5 | 7 |
| Fracture Toughness (Kicsr) (MPa m-1/2) 1304(T) | 1.6 | N/A | 0.2 | 0.25 | 0.5 |
| Polymerization Shrinkage(% linear) 4049(I) | 1.0 | N/A | 1.0 | 1.5 | (-) 0.4 |
| VHN Surface Hardness @ 3mm 4049(I) / 27(A) | 93 | 60 | 20 | 30 | 40 |
| Depth of Cure (mm) 4049(I) / 27(A) | 10.2 | 2.0 | N/A | N/A | N/A |
| Film Thickness, Microns (ìm) | 5 | 40 | 75 | 50 | 40 |
| Water Sorption (%wt.) (µg/cm3) 4049(I) / 27(A) | 0.7 | 1.7 | > 5 | > 3 | > 8 |

Cure Kinetics, Tw, Tg, Ts [ Work(w), Gel(g), Set(s)  - Time] - Min’ Sec’’  @  370C             3107(I)/ 8(A)/ 9(A)

Self/Auto Cure Mode (Catalyst + Base) (1:1 Ratio)

Tw - 1’00’’

Tg - 1’30’’

Ts - 2’30’’

1’00’’minima-

5’00’’maxima-

9’00’’maxima

1’30’’

4’00”

8’00”

1’00’’

3’00”

7’00”

1’30’’

3’00”

| 8’00” |
| --- |
| Biocompatability 10993(I) / 41(A) | Excellent | Moderate | Moderate | Moderate | Reactive |
| Catastrophic Strength - Crown / Tooth - Abutment @ OCA(Occlusal Contact Area)(MPa) (D) | 231 | 50 | 50 | 75 | 100 |
| Cytotoxicity (%) 10993(I) / 41(A) | 0 | 40 | 40 | 40 | 60 |

Resin-Matrix                                                            (D)

Filler

|  | Crystalline -PEX |
| --- | --- |

N/A

|  | Phosphoric Acid/ Zinc-Phospho-Silicate | Carboxylic acid/ Silicates |
| --- | --- | --- |

Polyacrylic, Carboxylic& Tartaric acids

| Fl-PAl-Silicates |
| --- |
| Fluorescent (D) | Yes | N/A | No | No | No |
| Transparent(Clear) / Opaque(White) (D) | Transparent | N/A | Opaque | Opaque | Opaque |
| Synthetic Collagen (D) | Yes | N/A | No | No | No |

DiamondBond-001™

Features & Benefits

STANDARDS – SPECIFICATION #

ISO-4049 ~ 4049(I)

ISO-10993 ~ 10993(I)

ISO-3107 ~ 3107(I)

ADA-27 ~ 27(A)

ADA-8 ~ 8(A)

ADA-9 ~ 9(A)

ADA 41~ 41(A)

ASTM 1304 ~ 1304(T)

ASTM-ANSI F394-78 ~ F394-78(T)

DRM ~ (D)

** ZP(ZincPhosphate), PC(Polycarboxylate,

GI(Glass Ionomer) Cements - Bonded to

Porcelain Crown

*  DiamondCrown Cemented w/ DiamondLink2-F/C

Cement & DiamondBond-001 Adhesive

Single-Step, Self-Etch-Prime&Bond Universal Adhesive System

Cyclic Fatigue Resistant, High Fracture Toughness, Shock Absorbing

Exceptional Bond Strength(Tensile/Shear) and Integration for Maximum Adhesion to Multiple Substrates:  Dentin/Enamel/Composite/Ceramic/Alloys

Mimics the properties of Natural tooth Dentition, Synthetic Collagen Polypeptide Bond

Special Salicylic-Lactic Conditioner, Less Post-Operative Sensitivity, Dentin-Tissue Specific Targeted Chem-Engineering, Maintains Dentin Architectural Micro-Morphology

Delivers Long Lasting Superior Adhesion, both Bio-Chemical and Physico-Mechanical to Tooth Structure for Ultimate Longevity:  Negligible Sorption & Absence of Solubility

Ultra Low Film Thickness ; Tough & Thin Interface for Optimum Crown/Abutment Tooth Fit Integrity and/or Filling/Tooth Marginal Seal (Micro-Elastic)

Crown/Filling Superstucture Reinforcement thru Interfacial Bonding/Substrate Integration

Excellent Marginal Integrity, Low Shrinkage-Low Probability of Post-Operative Sensitivity Microgap / Microleakage/ Microbial Invasion - Free

Superb Color Stability, Stain Resistance and Accurate Esthetic Shade Match

Easy Access, infiltrates the Most Difficult Preps., Enhanced Contact Angle Wetability / Adaptation to Acute Transitional Prep. Line Angles

Delivery Systems, avail. In 3/ 7 cc Adhesive (Dual-Cure) & 7cc Conditioner; Visible Light &/or Auto-Cure for both Direct Fillings and Crown & Bridge Application.

Refractive-Index, Chameleon-Like Effect

Biocompatible & Non-Cytotoxic