- DRM LABORATORIES, INC.

- DIAMONDLITE

Universal Direct Dental Restorative Micro-Hybrid Composite - Anterior / Posterior Filling System.

- Visible Light Cure

+

- DIAMONDBOND

- Universal Dental Adhesive System    Dual - Cure

Enamel, Dentin, Metal and Ceramic

Visible Light Cure / Self Cure

-------------------------------------------------------------------------------------------------------------------------------

- Recommended for class I, II, III, IV, V and esthetic direct veneer restorations.

- Store at or below room temperature.

- Keep refrigerated to prolong shelf-life.

- PRECAUTIONARY REMARKS:

- AVOID THE FOLLOWING AGENTS / TECHNIQUES:

- Pumice containing oil or fluoride.

- Hemostatic agent ( Hemodent) containing Ferric Sulfate and / or Aluminum Chloride.

- Retraction cords impregnated with hemostatic agents containing Ferric Sulfate

and / or Aluminum Chloride.

- Thin retraction cords may lead to crevicular fluid hydrostatic flow and cervical

restorative site contamination throughout adhesive, composite placement process.

- Overcuring restorative may lead to post - operative sensitivity.

- Undercuring restorative, i.e; 20 sec. or less per layer and / or use of  VLC apparatus

generating less than 500 mW/cm2 at 450-550 nm wavelength band.

- Moisture or oil containing compressed air contamination.

-------------------------------------------------------------------------------------------------------------------------------

- Alcohol cleanse all instruments, mandrels, etc. to avoid multi- components cross - contamination.

- PREPARATION: USE CONSERVATIVE TOOTH PREPARATION METHODOLOGY:

- Rounded internal line angles, avoid sharp transitions - binding sites.

- Convergent axial walls.

- Smooth cavity floor.

- Do not bevel the occlusal margins.

- Chamfer  the interproximal gingival seat margin.

- Avoid diatoric forms, undercuts, channeling - mechanical retention methods.

- PREPARATION TECHNIQUE:

Prepare the restorative site.

Clean with plain pumice, rinse and dry.

Isolate with rubber dam, or  cotton rolls and thick plain non-impregnated retraction cord, wedge & secure with tooth matrix of choice as needed.

- CONDITIONING, PRIMING & BONDING

- STEP 1 : Conditioning

- ENAMEL & DENTIN

- Apply the DiamondLite Tooth Conditioning Gel, secure disposable luer lock needle tips onto the 37% orthophosphoric acid gel, place on enamel and dentin surfaces when needed.  Allow to react for 15 seconds while agitating gel with disposable brush tip / brush holder provided (avoid desiccation).

- Stepwise conditioning gel placement is ideal, start with enamel, and at the 15 sec. mark, place gel

on dentin, at the 30 sec. mark from baseline, remove

- Rinse and dry.

- STEP 2: Priming

- DENTIN

- Place 1:1 ratio of  DiamondBond Primer A & B into well tray, mix with the disposable brush tip /

holder provided and brush several consecutive coats ( 4-6) onto dentin surfaces.

- Apply a gentle jet of air, glossy surface texture.

- STEP 3: Bonding

- ENAMEL AND DENTIN

- VISIBLE LIGHT CURE METHOD

- Place 1 drop of DiamondBond Universal Adhesive Resin BASE  into a clean well tray provided.

 Place a thin layer of  DiamondBond BASE Adhesive Resin onto both the enamel & dentin with

a disposable brush tip / holder.

- Thin with a jet of air.

- Visible light curing for 30 seconds.

- SELF CURE METHOD

- Place 1 : 1 ratio ( 1 drop of each) of  DiamondBond Universal Adhesive Resin CATALYST  and

BASE  into a clean well tray provided.

- Mix with a fresh brush tip / holder in well tray for 10 seconds.

- Brush a thin layer of adhesive mixture onto enamel and dentin.

- Thin with jet of air.

- Allow 2.5 minutes to set.

- DUAL CURE METHOD

- Follow self cure instructions.

- Complete cure by visible light for 30 seconds.

- CERAMIC REPAIR SITE

- STEP 1

Prep. repair surface with diamond bur.

   Intraoral microsandblast with fine abrasive, the restorative site, or roughen with fine diamond

bur.

Rinse and dry.

- STEP 2

- Dispense a drop of DiamondLite Ceramo-Coupler into clean well tray provided.

- Brush a few (2-3) layers of DiamondLite Ceramo-Coupler onto sandblasted/abraded, cleaned

and dried ceramo-repair site.

- Dry with gentle air jet.

- STEP 3

- Proceed with DiamondBond Universal Adhesive Resin Layer Placement & follow;

a)  VLC method, or

b)  Self-cure method, or

c)  Dual-cure method

- STEP 4

- FILLING RESTORATIVE SITE

- Select the appropriate shade equivalent syringe of DiamondLite  Filling Material.

- Apply a layering technique bucco-Lingual (posterior) or stepwise increments (anterior)

light shades - up to 3.0 mm Layers.

- Dark shades - up to 2.0 mm Layers.

- Pat & condense, carve and contour using gentle pressure with the DRM stainless placement instrument provided.

- Avoid porosity inclusions.

- Visible light cure for 40 seconds per layer from each tooth aspect; buccal / facial, lingual, occlusal /

incisal and interproximal ( clear light propagating tooth wedges recommended).

Remove mylar strips, tooth matrix, crown clear form, cervical clear bands.

- TRIMMING, FINISHING & POLISHING - DIAMONDLITE

- Trim DiamondLite with 8-12 fluted carbides, fine diamonds, or white stones.

- Finish with 30 - fine fluted carbides.

- Polish with DiamondLite Polishing Discs secured onto mandrel provided ( safe-side; allows

interproximal access, pliable texture; allows flexible contouring, with the DiamondLite

Polishing  Paste.

- For Lingual grooves, occlusal developmental grooves, pits & fissures, gain access with soft bristle

brush wheels, cups or soft rubber; discs, cups, cones or points.

DRM Research Laboratories, Inc. 29 Business Park Drive, Branford, CT  06405

Tel. (203) 488 - 5555  Toll Free (888) DRM-BOND [376-2663]  Fax. (203) 488-2821

 Email drmbond@drmco.com

415-13 Rev B                                                                                                                                    ver. 052510